## Slide 1
Stochastic particle-level modeling of nanocluster formation and coarsening on surfaces: Cluster diffusion & coalescence
Jim Evans, Alex Lai, Da-Jiang Liu, Yong Han (theory), Patricia Thiel (expt.)
Dept. of Physics & Astronomy and Dept. of Mathematics, Iowa State University
Ames Laboratory – USDOE, Iowa State University
Funding: NSF grant CHE-1507223
KC Lai, D-J Liu, PA Thiel, JW Evans
J. Phys. Chem. C 122 (2018) 11334

## Slide 2
Stochastic lattice-gas model for nanocluster formation during deposition
Surface hopping rates:
h =  exp[-Eact/(kBT)]
where Eact depends on
local environment 
Deposition & various surface
diffusion processes involving
hopping to adjacent adsorption
sites forming a periodic lattice
occur stochastically with prescribed
rates (i.e., as Markovian Processes
with appropriate exponential
waiting time distributions)
 Analytic theory: rate equations; BCF deposition-diffusion equns; LSW & Smoluchowski equn (coarsening)
 KMC simulation where processes are implemented stochastically with probabilities proportional to rates
Lai et al. Chem. Rev. (2019) subm.
Evans et al. Surf. Sci. Rep. 61 (2006) 1

## Slide 3
OUTLINE
This talk will focus on two-dimensional systems:
single-atom high (2D) metal islands or nanoclusters (NCs) on flat metal surfaces
Formation, i.e., self-assembly, of NCs during deposition
(i.e., diffusion-mediated NC nucleation and subsequent growth by aggregation)
Q1. Size and spatial distribution for ensembles or arrays of NCs
Q2. Far-from-equilibrium growth structure of individual NCs
Post-deposition coarsening of NC ensembles/arrays via
Ostwald Ripening or Smoluchowski Ripening (NC diffusion & coalescence)
Q1. Ensemble-level evolution of NC size distribution (LSW, etc.)
Q2. Dynamics of individual NCs ( growth/decay in Ostwald Ripening;
       diffusion and coalescence in Smoluchowski Ripening )
For surface systems, clear separation of time scales between NC formation and NC coarsening.

## Slide 4
Rate Equation Formulation …mean-field (MF) versions by Zinsmeister, Venables,… from 1960’s
Ns = density of stable islands of size s > i (critical size); Nisl = s>i Ns = total density; N1 = adatom density
d/dt Ns = s-1 h N1 Ns-1 - s h N1 Ns where s = avg. capture number for s > i
gain loss …h = terrace atom hop rate
s
s-1
h
h
Scaling for large h/F  large sav ~ (h/F)i/(i+2) z with z=(i+1)/(i+2)  Ns  f(x = s/sav); s  c(x = s/sav)
 f(x) = f(0) exp[ 0<y<x dy ]
(2z-1) - c(y)
c(y) – z y
Bartelt and Evans PRB 54 (1996) 17352
Evans et al. Surf. Sci. Rep. 61 (2006) 1-128
RATE EQUN ANALYSIS OF ISLAND/NC SIZE DISTRIBUTION
Approach to scaling limit
…depends on /* where
* ~ (h/F)-2/(i+3) denotes
end of transient regime &
start of steady-state regime
Han, Gaudry, Oliveira, Evans
J Chem Phys 145 (2016) 211904
KMC
i = 1

## Slide 5
CAPTURE-ZONE AREA DISTRIBUTIONS: THEORY
Develop fundamental rate equation theory for population, NA, of CZs
of area A which must account for subtle spatial aspects of nucleation
NA = - + +
d
dt
X
A
Probability Q(A) to overlap Probability Pnuc(A) to nucleate
existing CZ of area A ? new island with CZ area A ?
Han, Li, Evans, J. Chem. Phys. 145 (2016) 211911; Li, Han, Evans, PRL 104 (2010) 149601.
Surface is tessellated into capture
zones (CZs) where islands grow by
capture of (most) atoms deposited
in their CZ  island growth rate
 CZ area  capture number.
Nucleation occurs predominantly
nearby CZ boundaries away from
islands (higher adatom density)
=Ft
<<1
=Ft
 0.1 ML

## Slide 6
SCALING FORM NA  g( = A/Aav) : THEORY, KMC
SMALL CZ AREAS: g()   controlled by probability
Pnuc(A) to create small CZ involves island nucleation
in the center of a group of existing nearby islands.
Han, Li and Evans PRL10, JCP16:  = 3 (i=0), 4.5 (i=1)
cf. Pimpinelli + Einstein PRL07,10:  = 2 (i=0), 3 (i=1)
versus KMC:  = 2.75-3 (i=0), 3.5-4 (i=1)
LARGE CZ AREAS: g()  exp(-bn) …with  << 1
Han, Li and Evans: …controlled by large Q(A) for large A ? n = 1.5 ? (i=1)
cf. Pimpinelli + Einstein: Gaussian tail n = 2 (heuristic FPE) …vs KMC n =2 ?
log-log plot
i = 1
i = 1

## Slide 7
JOINT PROBABILITY DISTRIBUTION (JPD): POINT ISLAND RESULTS
Mulheran & Robbie EPL 49 (2000) 617; Bartelt + JE PRB 66 (2002) 235410
= c(x)

## Slide 8
135 K
194 K 80 x 30 nm2
220 K 120 x 90 nm2
Equil.
Eq.
Eq.
Non-equilibrium growth shapes of NCs
Ag/Ag(111) Ag/Ag(100) Ag/Ag(110)
aspect ratio 3
25 x 25 nm2
Cox et al. (ISU) PRB 71 (2005) Frank et al. (Ulm + ISU) PRB 66 (2002) Han et al. (ISU) PRB 88 (2013), PRB 87 (2013)

## Slide 9
HOPPING BARRIER SELECTION: GENERAL AB-INITIO LEVEL TREATMENT
ETS
Einit
thermally activated hop
Eact = ETS - Einitial
h =  exp(-Eact/kT)
initial
state
final
state
transition
state (TS)
Key ingredient: Determine unconventional adatom interactions int(TS-ad) with one atom
at TS as well as conventional interactions int(initial-ad) with both atoms at adsorption sites.
JPCC 120 (2016) 28639; JPCL 6 (2015) 2194; NL 14 (2014) 4646; PRL 108 (2012) 216102; PNAS 108 (2011); PRB 84 (2011); JCP 135 (2011)
Initial State
Conventional
interactions
Transition state
Unconventional
interactions

## Slide 10
Ni on NiAl(110) @ 300-500 K
Han et al. J Chem Phys 135 (2011) 084706
STM
KMC
Ni + Al co-deposition on NiAl(110)
Han et al. PRL (2012) 216102 Duguet et al. PNAS 109 (2011) 989
Au (+ Ag) on Ag(100)
Han et al. JPCL 6 (2015) 2194; Nano Lett. 14 (2014) 4646
300 K
250 K

## Slide 11
Ostwald Ripening (OR) of 2D Ag islands on Ag(111) surfaces
166 min
332 min
300 K
Coarsening of 2D NC ensembles in fcc homoepitaxy
Reviews: Thiel, Shen, Liu, Evans J. Phys. Chem. C 113 (2009) 5047; Karina Morgenstern Phys. Stat. Sol. B 242 (2005) 773
Diffusion-limited OR
BASIC FEATURES OF OR:
Equilibrated island shapes  well-defined chemical potential (R) = () + /R
Gibbs-Thompson: adatom density equil. with island eq(R)  eq()[ 1 + /(kBT R)]
Diffusive mass flow from higher  & eq to  & eq lower via /t = D2(x)  0
Chernov Boundary Condition (BC) at island edges involves a kinetic coefficient K
Kinetic coefft K describes ease of attachment of diffusing atoms to island edges
For metal islands typically no attachment barrier  K =   Dirichlet BC  = eq
R = island “radius”
300 K

## Slide 12
Ostwald Ripening (OR) of 2D Ag
islands in Ag(110) for T < 220K
Han, Russell,… Thiel, Evans PRB 87, 155420 (2013)
Wang, Han, Walen,… Thiel, Evans PRB 88, 155434 (2013)
Initial study: Morgenstern et al. PRL 83 (1999) 1613
length
width
area
length
width
KMC with realistic
atomistic-level
Ag/Ag(110) model
KMC @190 K
STM
nm
190 K
Refined kinetic coefficients: K <  even if no energy barrier for attachment to step edges
which have few kinks (since incorporation of diffusion atoms into islands occurs at kinks)
Derivation: Coarse-graining of 2D discrete diffusion equn incorporating kinked steps
Lack of island shape equilibration  introduce partial chem. potentials for length vs width change
Ackerman & Evans SIAM MMS 9 (2011) 59; Zhao, Ackerman, JE PRB 91 (2015) 235411; Zhao, JE, Oliveira PRB 93 (2016) 165411 – step permeability

## Slide 13
n
Continuum diffusion equn BVP analysis for rates of growth/decay of islands
Narrower islands with higher partial chem. potentials shrink and transfer atoms to wider islands.
Focusing on “narrow” island 1: initial rate of decay from analysis of BVP: R1 = -0.0022 nm2/s
Experimental decay rate R1  -0.005 nm2/s BUT decay is highly stochastic as confirmed
by multiple KMC simulation trials showing K1 varying from -0.0015 to -0.0075 nm2/s

## Slide 14
Smoluchowski Ripening of 2D Ag islands in Ag(100) surfaces
Why SR versus OR? Diffusion of individual atoms at island edges is facile
on (100) surfaces. So NC diffusion mediated by edge diffusion is also facile.
100 x 100 nm2
300 K
ISU group PRL (1994), PRL (1996), JCP (1999)
Review: J. Phys. Chem. C 113 (2009) 5047
~8 hr
~0.5 hr
5.78
14.54
36.51
0.76
5.78
1.56
1.56
1.56
2D Ag cluster on Ag(100)
Cluster Diffusion via edge atom hopping
Dependence of cluster diffusion coefft.
on island size, N (measured in atoms)
DN  N-1.15 for 90 < N < 400 at 300 K
Pai et al. (ORNL) PRL (1997)
versus Mean-Field (MF) Theory  D  N-1.5
Pai et al. PRL (1997)
300 K

## Slide 15
Atomistic vs continuum modeling: 2D Ag islands on Ag(100)
Hopping Attempt Rate
Edge Diffusion Barrier
Corner Rounding Barrier
Strength of NN Attraction
:
MULLINS-TYPE CONTINUUM MODELING…
Step chemical potential:   * 
where  = curvature ~ s2 h, * = stiffness
Mass Flux: JPD  - PD s  + noise*
Vn = -s JPD  h/t = s PD s * s2 h + conserved noise*
JPD
Vn = normal
velocity
h
s
E(SR) = Ee +  + KES
“TAILORED” ATOMISTIC MODEL FOR EVOLUTION VIA EDGE ATOM HOPPING
 shape relaxation time eq  N2  L4; diffusion coefft. DN  N-3/2  L-3
L
Cluster size
N  L2 atoms
Liu & Evans PRB (2002); Lai et al. PRB (2017)
Herring, Mullins,.. for 3D deterministic analogue; Khare & Einstein, PRL (1995), PRB (1996) – stochastic theory

## Slide 16
Coalescence (sintering) of pairs of 2D Ag islands on Ag(100)
Benchmark analysis with no corner rounding barrier ( = 0): atomistic vs continuum modeling

5.2 x 5.2 + 4.5 x 4.5 nm2 clusters 13.0 x 13.0 + 11.5 x 11.5 nm2 clusters
Modeling with ab-initio thermodynamics …and kinetics !
So for  = 0 one has L4 (Mullins prediction), but for (Ag)  0.15 eV then   L2-3 (expt & KMC)
DFT used to catalogue dominant pair, trio,.. interactions (both conventional int. determining
thermodynamics, and “unconventional” interactions determining barriers for edge diffusion)
STM
KMC
Han, Stoldt, Thiel, Evans JPCC 120 (2016) 21617
Liu & Evans
PRB 66 (2002) 165407

## Slide 17
Diffusion of 2D metal clusters on metal(100) surfaces
Start here
End here
Example of simulated trajectory
for cluster of N = 36 atoms
Long history of theoretical analysis
Voter, PRB 34 (1986); SPIE 821 (1986)

Heinonen, Kopenen, Merikoski,
Ala-Nissila, PRL 82 (1999)

Lai et al. JCP 147 (2017) 201101; PRB
96 (2017) 235406, JPCC 122 (2018) 11334
Motivated by expt observations of
diffusion of large clusters from mid-90’s
Wen et al. (ISU) PRL 73 (1994) 2591
Pai et al. (ORNL) PRL 79 (1997) 3210
Ye & Morgenstern PRB 85 (2012) 045417
Focus here on the size-dependence
of cluster diffusivity …rich behavior
Lai et al. J. Chem. Phys. 147 (2017) 201101; PRB 96 (2017) 235406

## Slide 18
Cluster Sizes
This does not apply for , etc. nor , ,…
Aside: “Perfect Cluster Sizes” with unique ground state shapes

## Slide 19
D
Large Size Regime
A
C
Branches & Mechanisms
Cyclic Variation of
E
Comparison with Experiments
B
Size-Scaling
K. C. Lai, D.-J. Liu, J. W. Evans
Phys. Rev. B 96 (2017) 235406.
Overview of Results
Heinonen et al. PRL 82 (1999) noted
fast diffusion for Np +1 …slower for Np

## Slide 20
Effective Energy Barrier of Forming a New Edge
Breaks 1 Bond
Breaks 1 Bond
Breaks 1 Bond
New Edge
New Edge
Facile
Nucleation Mediated
(Before any of them moves back to the corner)
Mechanisms of Long Range Diffusion
Faster Diffusion
Slower Diffusion
e.g.
e.g.

## Slide 21
Facile Diffusion
Wandering through configuration space of ground states
Degeneracy at ground states:
Cluster Size
nth excited state

## Slide 22
Nucleation-Mediated Diffusion
Dissociation
of Dimer
Nucleation
Dissociation
of Dimer
Nucleation
1) Being excited from configuration space
2) Wandering through configuration space
3) Dropping back to configuration space

## Slide 23
Arrhenius Plot- Varying

## Slide 24
Facile Diffusion
Large size-scaling exponent
(cf. MF/continuum value of  = 1.5)
Size-Scaling Exponents of Facile Branch
 |  | 2.60
 |  | 2.49
 |  | 2.60
 |  | 2.49

## Slide 25
Size-Scaling of Facile Branch,
Facile
Long range diffusion requires return to special configuration after
wandering through a large phase space of ground state configurations
From the theory of random walks/first-passage times,
the average time for a wandering through a large phase space and
returning to the same configuration
(E. W. Montroll J. Math. Phys. 1965)
How to find ?

## Slide 26
Counting Configurations:
Perimeter equivalent to energy of the system.
First analyze a simpler problem: determine the number of ways that
vacancies can be distributed at a single corner (creating a staircase).
This problem corresponds to analysis of integer partitions in number theory…
the different possible configurations correspond to Ferrer’s or Young’s diagrams
Solution of simpler problem leads to that of general problem (via convolution sums)

## Slide 27
Big Size-scaling exponent ,
 | 2.60
 | 2.49
 | 2.60
 | 2.49
 | 2.64
 | 2.74
 | 2.64
 | 2.74

## Slide 28
Cyclic Variation
= 42 + 7
are not the slowest sizes in a cycle.
increases as increases from to next biggest

## Slide 29
Requires excitation to diffuse
Nucleation-Mediated
Higher chance to be excited
Compare the between Nucleation Mediated cases
Higher
Trends for Nucleation Mediated Mechanism

## Slide 30
Cyclic Variation

## Slide 31
Transition to the Large Size Behavior
Matching mean-field model:
Smaller

## Slide 32
Pai et al. Phys Rev Lett 79, 3210 (97).
(Oak Ridge National Lab)
Ge, Morgenstern Phys. Rev. B 85, 045417 (2012).
ISU Experimental Data
(From Thiel group)
Experimental results not completely consistent.
Our conclusion:
Pits and islands have similar
ORNL results give most precise magnitude of .
Pit
Islands
Pits
Comparison with Ag(100) Experiments

## Slide 33
 clusters diffuse faster than pits (for same N)
…clusters & pits have similar diffusivity
Large  clusters diffuse slower than pits (for same N)
Pai et al. Phys Rev Lett 79, 3210 (97).
(From Oak Ridge National Lab)
Ge, Morgenstern Phys. Rev. B 85, 045417 (2012).
ISU Experimental Data
(From Prof. Thiel’s group)
Close symbol
Open symbol
Island
Pit
Comparison with Ag(100) Experiments






KMC Simulations
Lai et al. J. Phys. Chem. C 122, 11334 (2018)

## Slide 34
SUMMARY
NC formation or self-assembly (by diffusion-mediated nucleation & growth):
Realistic predictive atomistic modeling is now possible to describe individual non-
equilibrium NC shapes, but fundamental questions remain at the “ensemble level”
…exact theory for NC size distribution, CZ area distribution, JPD of NC size & CZ area
Coarsening of ensembles of NCs on surfaces:
 2D islands on perfect flat crystalline surfaces (especially metal homoepitaxy)
provides “ideal examples” of Ostwald Ripening and Smoluchowski Ripening,
but also reveal “anomalous” OR for anisotropic surfaces (unequilibrated islands)
Size dependence of cluster diffusivity provides key input to Smoluchowski’s
coagulation equations to describe SR kinetics. Behavior for moderate sizes
N = 10-100 is rich with distinct branches (facile vs nucleation-mediated),
diverse size scaling, oscillations, etc. elucidated through combinatorial analysis
Alex Lai Da-Jiang Liu Yong Han Pat Thiel

## Slide 35
Counting Configurations:
Consider each corner separately:
For a corner with vacancies.
Number of possible configuration:
Found by number theory
(Integer partition, Young’s diagram)
P(4) = 5

## Slide 36
Counting Configurations:
Put four corners back together.
4)
1) Draw a inscribing rectangle corresponding to the target energy. 2) Fill the rectangle with all adatoms.
3) Consider each corner separately:
s
e.g.

## Slide 37
Pit Diffusion: Avoiding
Some of the pathways not involving

## Slide 38
~50,000 atom single-layer
Ag nanocluster on Ag(111)
decays completely in ~7 min
with trace amounts of S (0.01ML)
versus ~30 hr no S at 300 K
…similar accelerated
decay of Cu islands on
Cu(111) induced by trace S
Ling, Bartelt, et al. PRL (2004)
See also: Feibelman PRL (2000)
~70 nm
Liu, Lee, Windus, Thiel, and Evans, Surf. Sci. 676 (2018) 2-8
Walen et al (ISU) PRB 71 (2015); Evans & Thiel, Science 330 (2010)
cf. Pt catalyst degradation/sintering: mass transport by PtO2 for Pt NP - PJF Harris, Int. Mat. Rev. 1995; Abild-Pederson et al. ACS Catal 6 (2016)
Accelerated nanocluster decay: trace S + M/M(111) for M = Ag, Cu
Analysis via linearization of coupled non-linear reaction-diffusion equations for formation,
dissolution and surface diffusion of complexes (as shown below assuming Cu2S3 dominates)
linearize
= metal atom
= sulfur atom

## Slide 39
Metal-S complexes on (111) surfaces of Ag, Cu, Au
LG modeling: long-range pair repulsions
(strain) + linear trio attractions
J Chem Phys (2013)
Russel, Da-Jiang Liu,
Y. Kim, Evans, Thiel
S on Ag(111)
S on Cu(111)
PRB (2015) Walen, Da-Jiang Liu, et al.
Surf Sci (2018) Liu, Lee... Thiel, Evans
S on Au(111)
JCP (2015) Walen, Da-Jiang Liu,..
cf. Reuter, Busnengo,… JPCC (2014)
S-M-S motif common for M = Ag, Cu
STM
DFT
DFT
STM
STM
DFT

## Slide 40
Sintering of metallic
NP with realistic surface
surface diffusion kinetics
ASSEMBLY & STABILITY OF METALLIC NANOCLUSTERS
Alex (King) Lai
Reshaping of cubic NP’s:
Diffusion of supported 3D NP’s:
N = 244 N = 269